


�





��












�



Bouwelven 1


B - 2280  Grobbendonk


Belgium





Tel.  +32 14 230001


Fax  +32 14 230880


�
�






4.	AWLGRIP PAINT SYSTEM FOR ALUMINUM SUBSTRATES


 	(WITH 545 PRIMER)�PRIVATE ��








SURFACE BELOW THE WATERLINE:





4.1.	Thoroughly degrease the surface using Surface Cleaner T-340.


	Grind with 36 grit sandpaper or sandblast to bare aluminium.


If necessary acid wash the surface with Deoxidine.


Wash in sections starting from the lower sections and working upwards.


Do not let the Deoxidine dry and rinse thoroughly with water.


This is most important !


When the substrate is completely dry proceed.





4.2.	Prime immediately with Awlgrip 545 Anti-Corrosive Epoxy Pri�mer Gray. Allow 2 hours minimum between coats at 20°C.  Allow to cure 12 - 14 hours.





		Base				: Gray  D1001 


		Converter			: D3001


		Reducer			: up to 25 % T0006 (min. 10 % T0006)


 		Induction time			: 15 minutes


		Recommended film thickness	: ± 250 micron wet = 75 micron dry


						  	  (calculated for mixed base and converter 


							  reduced 25 %)


	


	Sand with 80 - 120 grit paper.  Do not break through to bare metal!  Should you break through, reprime these areas immediately with Awlgrip 545 Gray Primer.





4.3.	Apply by trowel, as necessary, AwlFair Trowelable Fairing Compound Light Weight:





		Base				: D8020 White


		Converter			: D7007 Red   


		Mixing ratio			: 1/1 by volume


		Color				: pink


		Induction time			: no induction period needed


		Potlife				: 30 - 45 minutes





Mix by volume 1 part D8020 with 1 part D7007 converter. Mix well until a uniform pink color is obtained. Mixing must be thorough to insure a good cure. Awlfair can be sanded after a drying period of 24 hours at 20°C. Blocksand the Fairing Compound with grit 40, 60 or 80 in between the coats and before each next step.  Remove all sanding residue with clean dry compressed air before each next step.


Before proceeding to next coat, make sure no surface contamination is present.





Do not add thinners or reducers to the Awlfair Fairing Compound !














�





�


�












�
Bouwelven 1


B - 2280  Grobbendonk


Belgium





Tel.  +32 14 230001


Fax  +32 14 230880


�
�






4.4.	Cover the fairing system with one coat of Awlgrip Hull-Gard ER Epoxy Pri�mer. Hull-Gard ER can be applied by roller or spray:


                      


		Base plus Converter		: 73057


 		Mixing ratio			: 9/1 by volume


		Reducer			: not necessary - however if  wanted not more 						  than 10% T0006 in volu�me.


		Induction time			: 30 minutes


		Recommended film thickness	: 150 micron wet = 75 micron dry


		Color				: yellow





Roller application requires at least 2 coats.  Allow a drying time of 3 hours at 20°C in between coats.





Allow a drying time of minimum 3 hours / maximum 8 weeks at 20° C before proceeding. If 8 weeks are exceeded, please contact your U.S. Paint representative.





4.5.	Apply Hull-Gard WB in multiple coats up to a total dry film thickness of 400 micron. 2 to 4 coats may be required depending upon reduction and method of application. Allow a minimum of 5 hours and maximum of 24 hours at 20°C. between coats. 





		Base plus Converter		: Black 73152


						  White 73128


		Mixing ratio			: 4/1 by volume


		Reducer			: not necessary - however if wanted not more 


						  than 20% T0006 in volume 


		Induction time			: 15 minutes


		Recommended film thickness	: 200 micron wet = 150 micron dry.





The total thickness of Hull-Gard WB should be minimum 300 micron dry !





4.6.	Apply Anti-Fouling according to the directions of the manufacturer.








Note : In case no fairing is required, after step 4.2. (application of 545 Primer), one can


           proceed with step 4.4. (application of Hull-Gard ER). In between 545 Primer and 


           Hull-Gard ER allow overcoating time of 12 hours minimum and 24 hours maximum at


          20°C.   If the overcoating time of 24 hours is exceeded the 545 Primer needs to be 


          sanded with grit 100-150 prior to the application of the Hull-Gard ER.





                                                         





U.S. Paint - 09.10.1998











