


�





�


�












�
   


   


Bouwelven 1


B - 2280  Grobbendonk


Belgium





Tel.  +32 14 230001


Fax  +32 14 230880�
�



14.	 AWLGRIP PAINT SYSTEM FOR COMPOSITE PEEL-PLY SUBSTRATES








SURFACE ABOVE THE WATERLINE





14.1.	Immediately after removal of the Peel-Ply, Hull-Gard ER Epoxy Primer has to be applied.


	


It is important to apply the Hull-Gard ER directly after removal of the Peel-Ply as it is nearly impossible to degrease the surface with the two-cloth method prior to sanding.  Reason for this is that the composite surface is to rough to allow this.  Please contact your nearest Awlgrip distributor or U.S. Paint head office in case of difficulties or advise on the above matter !





As composite substrates vary in composition and in order to be sure that the underneath described Awlgrip paintsystem is suitable for the Peel-Ply substrate at issue, it is highly recommended to perform an adhesion tests with Hull-Gard ER Epoxy Primer prior to the application of the Awlgrip system !








14.2.	Apply one coat of Awlgrip Hullgard ER Epoxy Pri�mer. Hull-Gard ER can be applied by roller or spray:


                      


		Base plus Converter		: 73057


 		Mixing ratio			: 9/1 by volume


		Reducer			: not necessary - however if


				  		  wanted not more than 10% T0006 in


						  volu�me.


		Induction time			: 30 minutes


		Recommended film thickness	: wet 150 micron = 75 micron dry.


		Color				: cream





Roller application requires at least 2 coats.  Allow a drying time of 3 hours / 8 weeks at 20°C before proceeding.  If 8 weeks are exceeded, please contact your U.S. Paint representative.


 


Allow a minimum drying time of 3 hours at 20°C before proceeding.















































�





��












�
   


   


Bouwelven 1


B - 2280  Grobbendonk


Belgium





Tel.  +32 14 230001


Fax  +32 14 230880


  �
�






14.3.	Apply by trowel, as necessary, AwlFair Trowelable Light Weight Fairing Compound.





		Base				: D8020 White


		Converter			: D7007 Red


		Mixing ratio			: 1/1 by volume


		Color				: pink


		Induction time			: no induction period needed


		Potlife				: 30 - 45 minutes








Mix by volume 1 part D8020 base with 1 part D7007 converter. Mix well until a uniform pink color is obtained. Mixing must be thorough to insure a good cure. Awlfair can be sanded after a 


drying period of 24 hours at 20°C. Blocksand the Fairing Compound with grit 40, 60 or 80 in between the coats and before each next step.  Remove all sanding residue with clean dry compressed air.


Before  proceeding to next coat, make sure no surface contamination is present.





Do not add thinners or reducers to the Awlfair Fairing Compound!








14.4.	Apply one layer of Ultra-Build Epoxy Primer in 2 or 3 coats with a drying time in between the coats of minimum 2 hours and maximum 12 hours at a temperature of 20°C. 





		Base White			: D8008


		Converter			: D3018


		Mixing ratio			: 1:1 in volume


		Reducer			: 5-10% with T0073


		Induction time			: 15 minutes after mixing


		Recommended film thickness	: 625 - 750 micron wet = 375 - 500 micron dry


		 


After drying sand the surface with 120 grit sand paper. Remove all sanding residue with clean dry compressed air and use Surface Cleaner T340 and in case of high humidity / dew point Awl-Prep T0008 to clean the surface.  Use the two cloth method.  Make sure no oily type of contamination is present.





14.5.	Apply one coat of Awlgrip 545 Anti-Corrosive Epoxy Primer Gray or White.





		Base				: White D8001


						  Gray  D1001


		Converter			: D3001


		Reducer			: up to 25% T0006 (min. 10 % T0006)


 		Induction time			: 15 min.


		Recommended film thickness	: wet 175 - 250 micron = 50 - 75 micron dry


      					  	  (calculated for mixed base and converter


						  reduced 25%)














�





�


�












�
   


   


Bouwelven 1


B - 2280  Grobbendonk


Belgium





Tel.  +32 14 230001


Fax  +32 14 230880�
�






If necessary in order to cover sanding scratches, more coats can be applied. Allow a drying time of minimum 8 hours and maximum 24 hours at 20°C. in between the coats.  		





Sand the 545 Primer with 220-400 grit paper. This is necessary to provide a smooth surface for topcoat application.


Remove all sanding residue with clean dry compressed air and use Surface Cleaner T340 and in  case of high humidity / dew point T0008 to clean the surface.  Use the two cloth method. Use Awlgrip 73009 Premium Tack-Rags prior to topcoating. Check the cleaned surface.








14.6.	To obtain gloss, depth, and complete coverage apply Awlgrip Topcoat as follows:





Using recommended spray equipment, apply a light, smooth, slightly wet tack coat to the surface.  Allow tack coat to ‘flash off’ 30 to 45 minutes.  Then apply a full coat to achieve color coverage (i.e. hide) and film thickness requirements.  If preferred, three coats may be used.  Allow the second coat to ‘flash off’ 30 to 45 minutes until only slightly tacky before applying third coat.





Topcoating cannot be done in one coat!





		Base				: See color card


		Converter			: G3010


		Mixing ratio			: 1/1 by volume


 		Reducer			: ± 25% T0001 below 21°C.


						  ± 25% T0003 above 21°C.


 		Induction time			: 15 minutes


		Recommended film thickness	: 150 - 200 micron wet = 50 - 75 micron dry








For application of Awlgrip Topcoat by brush : 





	Base	: see color card


	Converter	: H3002


	Mixing ratio	: 2/1 by volume


	Reducer	: 10-20% T0031 


	Induction time 	: 15 minutes


	Recommended filmthickness: wet 100 - 150 micron = 50 - 75 micron dry





	Do not paint below a temperature of 18° C !








Note : Some colors may require more than 75 micron of dry film to achieve full hide or   


                 opacity, extra coats may be needed to achieve a dry film thickness greater than  


                 75 micron.


                                                      





		U.S. PAINT - 09.10.1998 	











