


�





��












�
   


Bouwelven 1


B - 2280  Grobbendonk


Belgium





Tel.  +32 14 230001


Fax  +32 14 230880


�
�






7.	AWLGRIP  PAINT SYSTEM FOR NON-ANODIZED ALUMINUM MASTS





7.1. 	Thoroughly clean and degrease the surface using Surface Cleaner T340.


	Sand the surface by using Scotchbrite together with Deoxidine.


	After maximum 4 minutes rinse the surface thoroughly with water.


	Do not let the Deoxidine dry !


	This is very important !





Caution :


Allow the mast to dry thoroughly.  Remove all dust from seams, joints, etc. with compressed air prior to proceed subsequent painting job.





7.2.	Prime immediately with 30-Y-94 Non-Sanding Mil-Spec Anti-Corrosive Epoxy Primer.





			Base				: S9001


			Converter			: S3001


			Mixing ratio			: 1/1 by volume


			Reducer			: 50 % T0006


			Induction time			: 15 minutes


			Recommended film thickness	: 75 micron wet = 20 micron dry.





	Allow the 30-Y-94 primer to dry for a minimum of 3 hours at 20°C.  Mil-Spec 30-Y-94 Primer must be overcoated within 3 - 6 hours of application.  Do not sand the Mil-Spec 


	30-Y-94 Primer !





7.3.	Apply Awlgrip 545 Anti-Corrosive Epoxy Pri�mer Gray or White. Allow 2 hours minimum between coats at 20°C.  Allow to cure 12 - 14 hours.





		Base				:Gray  D1001 


						 White D8020


		Converter			: D3001


		Reducer			: up to 25 % T0006 (min. 10 % T0006)


 		Induction time			: 15 minutes


		Recommended film thickness	: 175 - 250 micron wet = 50 - 75 micron dry


						  	  (calculated for mixed base and converter 


							  reduced 25 %)


	


	Sand with 80 - 120 grit paper.  Do not break through to bare metal!  Should you break through, reprime these areas immediately with Awlgrip 545 Gray Primer.



































�





��












�
   


Bouwelven 1


B - 2280  Grobbendonk


Belgium





Tel.  +32 14 230001


Fax  +32 14 230880


�
�



7.4.	Apply by trowel, as necessary, AwlFair Trowelable Light Weight Fairing Compound.





		Base				: D8020 White


		Converter			: D7007 Red


		Mixing ratio			: 1/1 by volume


		Color				: pink


		Induction time			: no induction period needed


		Potlife				: 30 - 45 minutes





Mix by volume 1 part D8020 base with 1 part D7007 converter. Mix well until a uniform pink color is obtained. Mixing must be thorough to insure a good cure. Awlfair can be sanded after a 


drying period of 24 hours at 20°C. Blocksand the Fairing Compound with grit 40, 60 or 80 in between the coats and before each next step.  Remove all sanding residue with clean dry compressed air.


Before  proceeding to next coat, make sure no surface contamination is present.


	


Do not add thinners or reducers to the Awlfair Fairing Compound!





7.5.	Apply one coat of Awlgrip 545 Anti-Corrosive Epoxy Primer Gray or White.





			Base				: White D8001


							  Gray  D1001


			Converter			: D3001


			Reducer			: up to 25 % T0006 (min. 10 % T0006)


			Recommended film thickness: 175 - 250 micron wet = 50 - 75 micron dry


							   (calculated for mixed base and converter 


							   reduced 25 %)





If necessary in order to cover sanding scratches, more coats can be applied.  Allow a drying time of minimum 8 hours and maximum 24 hours at 20°C in between coats.





Sand the 545 with 220 - 400 gritpaper.  This is necessary to provide a smooth surface for topcoat application.  Remove all sanding residue with clean dry compressed air and use Surface Cleaner T340  and in case of high humidity / dew point Awl-Prep T0008 to clean the surface.  Use the two cloth method.  Use AwlGrip 73009 Premium Tack-Rags.  Check the cleaned surface.





7.6.	To obtain gloss, depth and complete coverage apply Awlgrip Topcoat as follows :


	


Using recommended spray equipment, apply a light, smooth, slightly wet tack coat to the surface.  Allow tack coat to ‘flash off’ 30 to 45 minutes.  Then apply a full coat to achieve color coverage (i.e. hide) and film thickness requirements.  If preferred, three coats may be used.  Allow the second coat to ‘flash off’ 30 to 45 minutes until only slightly tacky before applying third coat.





Topcoating can not be done in one coat !





�






�





�


�












�
   


Bouwelven 1


B - 2280  Grobbendonk


Belgium





Tel.  +32 14 230001


Fax  +32 14 230880


   �
�









			Base				: see color card


			Converter			: G3010


			Mixing ratio			: 1/1 by volume


			Reducer			: ±  25 % T0001 below 21°C


							  ±  25 % T0003 above 21°C


			Induction time			: none


			Recommended film thickness: 150 - 200 micron wet = 50 - 75 micron dry








For application of AwlGrip Topcoat by brush : 





	Base	: see color card


	Converter	: H3002


	Mixing ratio	: 2/1 by volume


	Reducer	: 10-20% T0031 


	Induction time 	: 15 minutes


	Recommended filmthickness: 100 - 150 micron = 50 - 75 micron dry





	Do not paint below a temperature of 18 °C !





SPECIAL NOTE :


Anodized aluminum





De-anodize the aluminum surface with a solution of 33 % Natrium Hydroxyde.


Treat the surface by washing the aluminum with the Natrium Hydroxyde for ± 10 min.


Do not let the Natrium Hydroxyde solution dry on the surface !!  Rinse thoroughly with plenty of fresh tapwater !





After this chemical treatment follow step 7.1





* Notes :


1) Some colors may require more than 75 micron of dry film to achieve full hide or opacity.     


    Please note, extra coats may be needed to achieve a dry film thickness greater than 75 


    micron.


2) In case no fairing is required, after step 7.3 (the application of the 545 Primer), one can         


    proceed with step 7.6. (the application of the Awlgrip Topcoat).





                                                                                              





U.S. Paint - 09.10.1998











