


�





�


�












�
   


   


Bouwelven 1


B - 2280  Grobbendonk


Belgium





Tel.  +32 14 230001


Fax  +32 14 230880


   �
�






10.	AWLGRIP SYSTEM FOR OLD & NEW POLYESTER BOATS


 	


	(ECONOMY SYSTEM)








SURFACE BELOW THE WATERLINE 





10.1.	New boats: Degrease the gelcoat very thoroughly with Surface Cleaner T340 and in case of high humidity / dew point with Awl-Prep T0008. Use the two cloth method.


Degreasing of a new boat is very important because the presence of an unmolding	agent can cause disengagement of the paint system.  Sand the gelcoat flat with sandpaper grit 100-150.


	After sanding clean the surface once again with Surface Cleaner T340 and in case of high humidity / dew point with Awl-Prep T0008. Use the two cloth method.





	Old boats: Remove all existing paint layers to obtain a bare gelcoat. Degrease the gelcoat very thoroughly with Surface Cleaner T340 and in case of high humidity / dew point with Awl-Prep T0008. Use the two cloth method.





It is recommended to apply one coat of Hullgard ER Primer by roller to fill in any porosity on the surface.





10.2.	Apply Hull-Gard ER Epoxy Primer in multiple coats up to a total dry film thickness of 300 micron. Allow a drying time of minimum 3 hours at 20°C. in between coats. Hull-Gard ER can be applied by roller or spray.





		Base plus Converter		: 73057


 		Mixing ratio			: 9/1 by volume


		Reducer			: not necessary - however if  wanted not more 						  than 10% T0006 in volu�me.


		Induction time			: 30 minutes


		Recommended film thickness


		per coat		 	: 150 micron wet = 75 micron dry


		Color				: yellow





Total dry film thickness must be 300 micron minimum !






































�





��












�
   


   


Bouwelven 1


B - 2280  Grobbendonk


Belgium





Tel.  +32 14 230001


Fax  +32 14 230880


�
�






10.3.	Apply Awl-Star Gold Label Anti-Fouling as soon as the last coat of Hull-Gard ER is barely tackfree (i.e. approximately 3-4 hours at 20°C.) but still soft enough to allow identation with a fingernail. If the Hull-Gard ER is allowed to cure past this point, renew the surface with a fresh coat of Hull-Gard ER and then apply the first coat of Awl-Star Gold Label Anti-Fouling.





Gold Label Anti-Fouling can be applied by brush, roller, conventional- or airless spray.





		Code				: BP201   Charcoal Black 


						  BP401   Medium Green


						  BP501   Light Blue


						  BP502   Deep Blue


						  BP701   Red 


            							  BP802   White Lightning  


 		Recommended film thickness	: 200 - 250 micron wet = 100 - 125 micron dry


       		Total recommended 


		film thickness			: 250 - 300 micron dry








In between the different coats of Awl-Star Gold Label Anti-Fouling a drying time of minimum 5 hours at 21°C must be respected.





Allow overnight drying time at a temperature of 21°C before launching.








                                                         





		U.S. PAINT - 09.10.1998 	                                                                                    � PAGE �2�    		  











