


�





��












�
   


   


Bouwelven 1


B - 2280  Grobbendonk


Belgium





Tel.  +32 14 230001


Fax  +32 14 230880


   �
�



12.	AWLGRIP SYSTEM FOR BARE / NEW WOOD


(MAXIMUM BARRIER SYSTEM)





SURFACE BELOW THE WATERLINE 





12.1.	Thoroughly sand the wood with 80-120 grit sandpaper. Blow off sanding dust and residue with clean, dry compressed air. Clean the surface using Surface Cleaner T340 and in case of high humidity / dew point Awl-Prep T0008. Use the two cloth method. Make sure no oily type of contamination is present.


	


12.2.	Seal the wood with Awlgrip 545 Anti-Corrosive Epoxy Pri�mer White. Allow the seal to cure 8-12 hours at 20°C. before recoating.  If more than 24 hours elapse, the seal coat must lightly be sanded with grit 180-220 grit paper before proceeding. Sealcoat of 545 Primer can be applied by brush, roller or spray method.





		Base				: White D8001


		Converter			: D3001


		Reducer			: Spray application	: 40 % with T0006


						  Brush application	: 40%  with T0031 


 		Induction time			: 15 minutes


		Recommended film thickness	: 175 - 250 micron wet = 50 - 75 micron dry


						  	  (calculated for mixed base and converter 


							  reduced 25 %)





12.3.	Apply Awlgrip 545 Anti-Corrosive Epoxy Pri�mer Gray or White. Allow 2 hours minimum between coats at 20°C.  Allow to cure 12 - 14 hours.





		Base				: Gray  D1001 


						  White D8001


		Converter			: D3001


		Reducer			: up to 25 % T0006 (min. 10 % T0006)


 		Induction time			: 15 minutes


		Recommended film thickness	:  175 - 250 micron wet = 50 - 75 micron dry


						  	  (calculated for mixed base and converter 


							  reduced 25 %)


	


	Sand with 80 - 120 grit paper.  Do not break through to bare wood!  Should you break through, reprime these areas immediately with Awlgrip 545 Gray Primer.





























�





��












�
   


Bouwelven 1


B - 2280  Grobbendonk


Belgium





Tel.  +32 14 230001


Fax  +32 14 230880


   �
�






12.4.	Apply by trowel, as necessary, AwlFair Trowelable Fairing Compound Light Weight:





		Base				: D8020 White


		Converter			: D7007 Red   


		Mixing ratio			: 1/1 by volume


		Color				: pink


		Induction time			: no induction period needed


		Potlife				: 30 - 45 minutes





Mix by volume 1 part D8020 with 1 part D7007 converter. Mix well until a uniform pink color is obtained. Mixing must be thorough to insure a good cure. Awlfair can be sanded after a drying period of 24 hours at 20°C. Blocksand the Fairing Compound with grit 40, 60 or 80 in between the coats and before each next step.  Remove all sanding residue with clean dry compressed air before each next step.





Before proceeding to next coat, make sure no surface contamination is present.





Do not add thinners or reducers to the Awlfair Fairing Compound !








12.5.	Cover the fairing system with one coat of Awlgrip Hull-Gard ER Epoxy Pri�mer. Hull-Gard ER can be applied by roller or spray:


                      


		Base plus Converter		: 73057


 		Mixing ratio			: 9/1 by volume


		Reducer			: not necessary - however if  wanted not more 						  than 10% T0006 in volu�me.


		Induction time			: 30 minutes


		Recommended film thickness	: 150 micron wet = 75 micron dry


		Color				: yellow





Roller application requires at least 2 coats.  Allow a drying time of 3 hours / maximum 8 weeks at 20°C before proceeding.  If 8 weeks are exceeded, please contact your U.S. Paint representative.





Allow a drying time of minimum 4 hours at 20° C before proceeding.






































�





��












�
   


   


Bouwelven 1


B - 2280  Grobbendonk


Belgium





Tel.  +32 14 230001


Fax  +32 14 230880


   �
�



12.6.	Apply Hull-Gard WB in multiple coats up to a total dry film thickness of 400 micron. 2 to 4 coats may be required depending upon reduction and method of application. Allow a minimum of 5 hours and maximum of 24 hours at 20°C. between coats. 





		Base plus Converter		: Black 73152


						  White 73128


		Mixing ratio			: 4/1 by volume


		Reducer			: not necessary - however if wanted not more 						  than 20% T0006 in volume 


		Induction time			: 15 minutes


		Recommended film thickness	: 200 micron wet = 150 micron dry.





The total thickness of Hull-Gard WB should be minimum 300 micron dry !





12.7.	Apply Awl-Star Gold Label Anti-Fouling as soon as the last coat of Hull-Gard WB is barely tackfree (i.e. approximately 3-4 hours at 20°C.) but still soft enough to allow identation with a fingernail. If the Hull-Gard ER is allowed to cure past this point, renew the surface with a fresh coat of Hull-Gard ER and then apply the first coat of Awl-Star Gold Label Anti-Fouling.





Gold Label Anti-Fouling can be applied by brush, roller, conventional- or airless spray.





		Code				: BP201   Charcoal Black 


						  BP401   Medium Green


						  BP501   Light Blue


						  BP502   Deep Blue


						  BP701   Red 


            							  BP802   White Lightning  


 		Recommended film thickness	: 200 - 250 micron wet = 100 - 125 micron dry


       		Total recommended 


		film thickness			: 250 - 300 micron dry








In between the different coats of Awl-Star Gold Label Anti-Fouling a drying time of minimum 5 hours at 21°C  must be respected.





Allow overnight drying time at a temperature of 21°C before launching.





Note : In case no fairing is required, after step 12.3. (application of 545 Primer), one can proceed with step 12.5. (application of Hull-Gard ER). In between 545 Primer and Hull-Gard ER allow overcoating time of 12 hours minimum and 24 hours maximum at 20°C.


If the overcoating time of 24 hours is exceeded the 545 Primer needs to be sanded with grit 100-150 prior to the application of the Hull-Gard ER.


                                                         





		U.S. PAINT - 09.10.1998	














