


�





��












�
   


   


Bouwelven 1


B - 2280  Grobbendonk


Belgium





Tel.  +32 14 230001


Fax  +32 14 230880


�
�



11.	AWLGRIP SYSTEM FOR BARE / NEW WOOD








SURFACE ABOVE THE WATERLINE 





11.1.	Thoroughly sand the wood with 80-120 grit sandpaper. Blow off sanding dust and residue with clean, dry compressed air. Clean the surface using Surface Cleaner T340 and in case of high humidity / dew point Awl-Prep T0008. Use the two cloth method. Make sure no oily type of contamination is present.





	


11.2.	Seal the wood with Awlgrip 545 Anti-Corrosive Epoxy Pri�mer White. Allow the seal to cure 8-12 hours at 20°C. before recoating.  If more than 24 hours elapse, the seal coat must lightly be sanded with grit 180-220 grit paper before proceeding. Sealcoat of 545 Primer can be applied by brush, roller or spray method.





		Base				: White D8001


		Converter			: D3001


		Reducer			: Spray application	: 40 % with T0006


						  Brush application	: 40%  with T0031 


 		Induction time			: 15 minutes


		Recommended film thickness	: 175 - 250 micron wet = 50 - 75 micron dry


						  	  (calculated for mixed base and converter 


							  reduced 25 %)


	





11.3.	Apply Awlgrip 545 Anti-Corrosive Epoxy Pri�mer Gray or White. Allow 2 hours minimum between coats at 20°C.  Allow to cure 12 - 14 hours.





		Base				: Gray  D1001 


						  White D8001


		Converter			: D3001


		Reducer			: up to 25 % T0006 (min. 10 % T0006)


 		Induction time			: 15 minutes


		Recommended film thickness	:  175 - 250 micron wet = 50 - 75 micron dry


						  	  (calculated for mixed base and converter 


							  reduced 25 %)


	


	Sand with 80 - 120 grit paper.  Do not break through to bare wood!  Should you break through, reprime these areas immediately with Awlgrip 545 Gray Primer.


























�





�


�












�
   


   


Bouwelven 1


B - 2280  Grobbendonk


Belgium





Tel.  +32 14 230001


Fax  +32 14 230880


  �
�



11.4.	Apply by trowel, as necessary, AwlFair Trowelable Fairing Compound Light Weight:





		Base				: D8020 White


		Converter			: D7007 Red   


		Mixing ratio			: 1/1 by volume


		Color				: pink


		Induction time			: no induction period needed


		Potlife				: 30 - 45 minutes





Mix by volume 1 part D8020 with 1 part D7007 converter. Mix well until a uniform pink color is obtained. Mixing must be thorough to insure a good cure. Awlfair can be sanded after a drying period of 24 hours at 20°C. Blocksand the Fairing Compound with grit 40, 60 or 80 in between the coats and before each next step.  Remove all sanding residue with clean dry compressed air before each next step.





Before proceeding to next coat, make sure no surface contamination is present.





Do not add thinners or reducers to the Awlfair Fairing Compound !





11.5.	Apply one layer of Ultra-Build Epoxy Primer in 2 or 3 coats with a drying time in between the coats of minimum 2 hours and maximum 12 hours at a temperature of 20°C. 





		Base White			: D8008


		Converter			: D3018


		Mixing ratio			: 1:1 in volume


		Reducer			: 5-10% with T0073


		Induction time			: 15 minutes after mixing


		Recommended film thickness	: 625 - 750 micron wet = 375 - 500 micron dry


		 


After drying sand the surface with grit 120.  Remove all sanding residue with clean dry compressed air thoroughly and use Surface Cleaner T340 and in case of high humidity / dew point Awl-Prep T0008 to clean the surface. Use the two cloth method. Make sure no oily type of contamination is present.





11.6.	Apply one coat of Awlgrip 545 Anti-Corrosive Epoxy Primer Gray or White.





		Base				: White D8001


						  Gray  D1001


		Converter			: D3001


		Reducer			: up to 25% T0006 (min. 10 % T0006)


 		Induction time			: 15 minutes


		Recommended film thickness	: 175 - 250 micron wet = 50 - 75 micron dry


	      					  (calculated for mixed base and converter 


						   reduced 25%)





If necessary in order to cover sanding scratches, more coats can be applied. Allow a drying time of minimum 8 hours and maximum 24 hours at 20°C. in between the coats. 		








�





�


�












�
   


   


Bouwelven 1


B - 2280  Grobbendonk


Belgium





Tel.  +32 14 230001


Fax  +32 14 230880�
�



			  


Sand the 545 Primer with 220-400 grit paper. This is necessary to provide a smooth surface for topcoat application.


Remove all sanding residue with clean dry compressed air and use Surface Cleaner T340 and in case of high humidity / dew point Awl-Prep T0008 to clean the surface.  Use the two cloth method. Use Awlgrip 73009 Premium Tack-Rags prior to topcoating. Check the cleaned surface.


	


11.7.	To obtain gloss, depth, and complete coverage apply Awlgrip Topcoat as follows:





Using recommended spray equipment, apply a light, smooth, slightly wet tack coat to the surface.  Allow tack coat to ‘flash off’ 30 to 45 minutes.  Then apply a full coat to achieve color coverage (i.e. hide) and film thickness requirements.  If preferred, three coats may be used.  Allow the second coat to ‘flash off’ 30 to 45 minutes until only slightly tacky before applying third coat.





Topcoating cannot be done in one coat!





		Base				: see color card


		Converter			: G3010


		Mixing ratio			: 1/1 by volume


 		Reducer			: ± 25% T0001 below 21°C.


						  ± 25% T0003 above 21°C.


 		Induction time			: 15 minutes


		Recommended film thickness	: 150 - 200 micron wet = 50 - 75 micron dry








For application of Awlgrip Topcoat by brush : 





	Base	: see color card


	Converter	: H3002


	Mixing ratio	: 2/1 by volume


	Reducer	: 10-20% T0031 


	Induction time 	: 15 minutes


	Recommended filmthickness: wet 100 - 150 micron = 50 - 75 micron dry








	Do not paint below a temperature of 18 °C !








Note : Some colors may require more than 75 micron of dry film to achieve full hide or 


                 opacity, extra coats may be needed to achieve a dry film thickness greater than 


                 75 micron.








                                                         





		U.S. PAINT - 01.04.1996	                                                                                    � PAGE �1�    			














